## Slide 1: Nuclear emulsions Slavic in 2012-13

## Slide 2: 1. IN BECQUEREL project
January 2012: 100 plates (9 cm x 12 cm, thickness emulsion layer ~ 100, µ Em.№: 14S, 20S, 21S)
November 2012: 50 plates (9 cm x 12 cm, thickness emulsion layer ~ 180, µ Em.№: 25S)
Mart 2013: 100 plates (9 cm x 12 cm, thickness emulsion layer ~ 100, µ Em.№: 30S)
June 2013: 100 plates (9 cm x 12 cm, thickness emulsion layer ~ 100, µ Em.№: 34S)
Emulsion was irradiated: neutrons 14MeV (DVIN); µ-mesons (CERN); 8He, Kr, Xe, 9C, 13O (JINR); Femtosecond laser (MOSCOW STATE UNIVERSITY) and many other works.
There were many reports about these works

## Slide 3: 2. Testing emulsion
In the period of 2012 - 13
we estimated 10 emulsion numbers
As an example the following tables are presented

## Slide 4
Обознач. образца | Дата Облуч. | Чем | Дата Обраб. | Прояв. | Режим | Толщина |  | Коэфф. усадки | Вуаль | Ионизация | Примечание
 |  |  |  |  |  | обр. слой | слой до обр |  |  |  | 
29_30С-1 | 06.03.2013 | мед p | 11.03.2013 | Ам | 20-20 | 64,8 | 115 | 1,77 | 0,80 | 48,60±3,03 | 
29_30С-2 | 06.03.2013 | мед p | 19.03.2013 | Ам | 20-20 | 62,80 | 115 | 1,83 | 0,78 | 45,70±3,74 | 
29_30С-3 | 17.03.2013 | пр. маркир | 18.03.2013 | Ам | 20-20 |  | 115 |  |  |  | не измерялось
29_30С-4 | 06.03.2013 | Хе | 18.03.2013 | Ам | 20-20 |  | 115 |  |  |  | не измерялось
29_30С-5 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 67,3 | 115 |  | 0,95 | 20,63±4,35 | 
29_30С-6 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 63,0 | 115 | 1,83 | 0,79 | 21,29±4,42 | 
29_30С-7 |  |  |  |  |  |  | 115 |  |  |  | пока не обрзботан
29_30С-8 |  | Bi | 18.03.2013 | Ам | 20-20 | 66,3 | 115 |  | 0,70 | 19,42±4,47 | 
28С-1 | 06.03.2013 | мед p | 11.03.2013 | Ам | 20-20 | 67,5 | 130 | 1,93 | 1,32 | 48,95±4,54 | 
28С-2 | 06.03.2013 | мед p | 18.03.2013 | Ам | 20-25 | 67,80 | 130 | 1,92 | 1,17 | 51,58±2,77 | 
28С-3 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 69,50 | 130 | 1,87 | 0,84 | 19,4±4,23 | 
28С-4 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 71,7 | 130 | 1,81 | 0,97 | 17,37±4,67 | 
28С-5 |  |  |  |  |  |  | 130 |  |  |  | пока не обрзботан
28С-6 |  | Bi | 19.03.2013 | Ам | 20-20 | 72,0 | 130 | 1,81 | 0,83 | 16,32±3,59 | 
Notes: Благодарности!

## Slide 5
Обозначение образца | Дата облучения | Чем | Дата обработки | Прояв. | Режим | Толщина |  | Коэфф. усадки | Вуаль | Ионизация | Примечание
 |  |  |  |  |  | обр. слой | слой до обр |  |  |  | 
29_30С-1 | 06.03.2013 | мед p | 11.03.2013 | Ам | 20-20 | 64,8 | 100 | 1,54 | 0,80 | 48,60±3,03 | 
29_30С-2 | 06.03.2013 | мед p | 19.03.2013 | Ам | 20-20 | 62,80 | 100 | 1,59 | 0,78 | 45,70±3,74 | 
29_30С-3 | 17.03.2013 | П маркир | 18.03.2013 | Ам | 20-20 |  | 100 |  |  |  | не измерялось
29_30С-4 | 06.03.2013 | Хе | 18.03.2013 | Ам | 20-20 |  | 100 |  |  |  | не измерялось
29_30С-5 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 67,3 | 100 | 1,49 | 0,95 | 20,63±4,35 | 
29_30С-6 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 63,0 | 100 | 1,59 | 0,79 | 21,29±4,42 | 
29_30С-7 |  |  |  |  |  |  | 100 |  |  |  | пока не обрзботан
29_30С-8 |  | Bi | 18.03.2013 | Ам | 20-20 | 66,3 | 100 | 1,51 | 0,70 | 19,42±4,47 | 
28С-1 | 06.03.2013 | мед p | 11.03.2013 | Ам | 20-20 | 67,5 | 130 | 1,93 | 1,32 | 48,95±4,54 | 
28С-2 | 06.03.2013 | мед p | 18.03.2013 | Ам | 20-25 | 67,80 | 130 | 1,92 | 1,17 | 51,58±2,77 | 
28С-3 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 69,50 | 130 | 1,87 | 0,84 | 19,4±4,23 | 
28С-4 | 17.03.2013 | d 4GeV | 19.03.2013 | Ам | 20-20 | 71,7 | 130 | 1,81 | 0,97 | 17,37±4,67 | 
28С-5 |  |  |  |  |  |  | 130 |  |  |  | пока не обрзботан
28С-6 |  | Bi | 19.03.2013 | Ам | 20-20 | 72,0 | 130 | 1,81 | 0,83 | 16,32±3,59 |